|  | ATLAS Pixel Stave TMT Specification for material procurement |  |  |
| --- | --- | --- | --- |
| ATLAS Project Document No: | ###### ABS item number | Created : 21.5.2001 | Page: 1 of 2 |
| ATL-IP-ES-0023 | ATL-0000005480 | Modified : 29.11.2001 | Rev. No .: v.1 |

| ATLAS Pixel Stave TMT Specification for material procurement: Carbon-Carbon |  |  |
| --- | --- | --- |
| Prepared by: K.W. Glitza | Checked by: | Approved by: |
| Distribution List |  |  |

Description: carbon-carbon (carbon fibres in carbon matrix), 2-D roving fabric layers overlapped in a phenolic resin matrix, densified and graphitized at high temperature.

Qualified suppliers:

SGL TECHNIK GMBH, type 1502 ZV 22

Physical properties:

| PROPERTY | UNIT | SPECIFICATION | TO BE CERTIFIED |
| --- | --- | --- | --- |
| Impurity | ppm | < 100 | * |
| Density | g/cm3 | 1,76 0.04 | * |
| Porosity | % | 13  2 |  |
| CTE – in plane | 10-6 K-1 | -0.5  0.2 @ 300°C |  |
| CTE – transverse | 10-6 K-1 | 12 1 @ 300°C |  |
| Kt – in plane | W/mK | 250  10 @ 20°C |  |
| Kt – transverse | W/mK | 30  3 @ 20°C | * |
| Young’s modulus-in plane | GPa | 120  20 | * |

Dimensions: plates 430x25x2.4 mm

Remarks:

Acceptance test as per procedure ATL-IP-QP-0015