| ASSEMBLY PROCEDURE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| polyimide heaters on atlas beampipe |  |  |  |  |  |
| Abstract This document describes how to mount the polyimide heaters on the ATLAS beampipe. |  |  |  |  |  |
| Prepared by : [Name] Hendrik KOS LHC/VAC [hendrik.kos@cern.ch] |  |  | Checked by : Raymond VENESS LHC/VAC |  |  |
| History of Changes |  |  |  |  |  |
| Rev. No. | Date | Pages |  | Description of Changes |  |
| 0 | 24.07.2002 |  |  | First release |  |

Table of Contents (not compulsory, can be removed)

1. Description of mounting heaters in nine steps	4

2. TWO ADDITIONAL STEPS FOR DOUBLE WALL OPTION……………………………9

OPERATION # A

Operation description

- Preparation inner tube.

- One extremity in manipulator, other extremity on rolling support.

- Make sure that the tube surface is clean and without sharp irregularities.

Resources required

- Manipulator.

- Rolling support.

OPERATION # B

Operation description

- Mounting heater.

- Attach heater to the tube with self adhesive tape and cable ties.

- Fill the gaps in between the heating patches with polyimide tape, glue side on the outside.

Resources required

- Polyimide tape, Pixeo Kaneka.

- Cable ties L=250.

- Gloves

- Heater, Rica.

- Polyimide self adhesive tape, Permapack P221.

OPERATION # C

Operation description

- Polyimide tape spirally wrapped around the tube, half overlapped. This gives two layers of polyimide tape around the heater.

- When wrapping polyimide tape, remove self adhesive tape and cable ties.

- The polyimide tape should never be glued to the tube, only to itself or to the polyimide heater.

Resources required

- Polyimide tape, Pixeo, Kaneka.

OPERATION # D

Operation description

- The polyester tape is wrapped spirally around the assembly. First 3 rotations straight, than with an angle to create a 50% overlap, giving two layers.

- At the extremities and also at every half a meter the polyester tape is attached by polyimide self adhesive tape.

Resources required.

- 30 mm polyester tape, Fratec 117803.

OPERATION # E

Operation description

- One layer of aluminized polyimide foil is wrapped around the assembly and attached by means of polyimide self adhesive tape.

- Ceramic spacers are taped around the tube with self adhesive tape with glass-cloth, to avoid thermal losses to the vacuum chamber.

- The distance between the spacers is 2.5 meters.

Resources required

- Aluminized polyimide, Tricon.

- Self adhesive tape with glass-cloth, 3M scotch 27.

- Ceramic spacers.

OPERATION # F

Operation description

- Heater connected electrically with flexible wire, polyimide, and ceramic connector blocks to electric feedthrough.

Resources required

- Flexible wire, polyimide, Habia H-H2419.

- Ceramic connector blocks.

- Electric feedthrough for vacuum chamber.

OPERATION # G

Operation description

- Elecrically test the circuits.

- Insert assembly into vacuum chamber.

- Thermocouples on the inside of the tube.

- Close vacuum chamber.

- Pump vacuum chamber down.

Resources required

- Vacuum chamber, inner diameter 100 mm+, 7.5 m+ long.

- Vacuum pumping station.

- 4 thermocouples, E-type.

- Thermocouple recorder.

- Multimeter.

OPERATION # H

Operation description

- First several hours of pumping, preferably overnight, to obtain a good vacuum.

- Start heating. Two times 150 V AC gives a stable 200° C.

- 200° C for 1 hour will cure the glue.

Resources required

- Two variable transformers. Each transformer feeds two serial linked circuits of the heater.

OPERATION # I

Operation description

- Stop Pumping.

- Let the tube cool down.

- Open vacuum chamber and take the assembly out.

- Take of the aluminized polyimide foil and ceramic spacers.

- Check visually if everything is OK.

- Electrically test circuits.

OPERATION # J  (For double wall option.)

Operation description

- Mount vespel spacers.

- Wrap two layers aluminized polyimide foil loosely around the tube.

- Cut small holes in the aluminized polyimide foil where the spacers touch the outer tube.

- Carefully insert the inner tube into the outer tube.

Resources required

- Vespel spacers

- Cutter.

- Polyimide strips cut out of a 0.15 mm foil, 2 mm wide, 300 mm long.

OPERATION # K  (For double wall option.)

Operation description

- Compress bellows 12 mm.

- Make sure that 4 wires protrude from each pumping port.

- Weld second flange on the inner tube.

- Release bellows compression tool.

- Check electric resistance of the polyimide heaters.

- Close pumping ports with KF covers.

Resources required

- Bellows compression tool.

- Welding equipment.

- Multimeter.

- KF covers.