## Slide 1
VOC Emissions Reduction from Photolithographic Processes
Dr. Thomas W. Peterson
Chemical and Environmental Engineering,
University of Arizona
 1999 Arizona Board of Regents for The University of Arizona

## Slide 2: Photolithography
Application and development of photoresist with the use of light and heat to write a pattern of microstructures on a wafer
Photoresist
  Protective material used to form a resistant film on the wafer surface
  Reacts chemically with areas exposed (not covered by a patterned mask) to become more or less soluble with respect to a solvent

## Slide 3: Basic Photo Process Steps
Notes: 4

## Slide 4: Spin-Coat Resist Usage/Waste
Notes: 5

## Slide 5: Chemical Usage in the Photolithography Process
Standard photoresist chemicals
  Resin (e.g. Cresol-formaldehyde {Novolac} )
  Solvents
    Ethyl lactate (EL) (b.p 154C)
    Ethyl 3-ethoxypropionate (EEP)
    Cellosolve Acetate
  Photo-active Compounds
Developer
Edge Bead Remover
Solvents
Notes: 6

## Slide 6: Strategies for Reducing VOC Emissions
Switch to Water-Based Resists
  Advantage: no VOC emissions
  Disadvantage: line width resolution, “speed”
Optimize Use of Current Solvent-Based Resists
  Advantage: utilize current formulations, equipment
  Disadvantage: no hope for eliminating VOC emissions
Notes: 7

## Slide 7: Benefits to Minimizing Resist Usage
Resist cost (~$500/gallon)
Environmental Impact
  Most of the Resist is “wasted”, in the sense that it is spun off the wafer. The high “waste” is required to achieve uniformity in thickness and proper coverage.
  Because of precise resist formulations, solvent evaporation during spinning, and contamination concerns, it is impossible to recycle resist that is spun from the wafer.
  Typically, Organic Solvents are used to clean the photoresist “cups” into which the excess resist is spun. Less solvent usage leads to less emissions of Volatile Organic Compounds (VOCs).
Notes: 8

## Slide 8: Photoresist Dispense Optimization
Objective
  Coverage of given thickness
  Coverage of given uniformity
Control Variable(s)
  Resist properties (viscosity, solvent mass fraction, amount dispensed)
  Spin speed
  Spin recipe
  Temperature, RH
Notes: 9

## Slide 9: Three Steps to Coating Process
Notes: 10

## Slide 10: Spin-Coat Operating Parameters
Spin Speed (rpm)
Spin Time (sec)
Surface Temperature
Room Temperature
Room Humidity
Resist Volume
Resist Viscosity
Resist Solid Mass Fraction
Notes: 11
11

## Slide 11: Properties of Photoresist
Initial Viscosity: 5 to 100 cP
Solvent Mass Fraction (SMF): 70-90%
Photoresist viscosity for the experiments presented:
  560 Resist - 17 cP
  500 Resist - 40 cP
Typical Viscosity Changes: 0.01 to 10,000 Poise as SMF goes from 1.0 to 0.0
Typical Diffusivity Changes: 10-6 to 10-12 cm2/sec as SMF goes from 1.0 to 0.0
Notes: 12

## Slide 12: Coating Process Overview
Current Practice
  At slow speed (usually ~2000 rpm) dispense 3-5 cc resist and spin for less than 2 seconds
  Ramp up speed (~3000 rpm) and spin for 20-30 seconds
  Apply Edge Bead Remover
  Fraction Resist “spun off”: typically 97-99%
Ultra Casting Pre-dispense (UCP)
  At very high speed (6000 rpm) dispense 1 cc resist and spin for 1 second
  Decelerate to 2000 rpm and apply second dispense of 1 cc
  Accelerate to 3000 rpm and spin for 20-30 seconds
  Apply Edge Bead Remover
  Fraction Resist “spin off”: typically 95-97%
Notes: 13

## Slide 13: How Fast Does the Solvent Evaporate?
Notes: 14
14

## Slide 14: Solid and Solvent Mass Remaining on Wafer
Notes: 15

## Slide 15: Flow Characteristics: Resist Dispense Nozzle
Notes: 16

## Slide 16: Resist Flows vs. Pressure Drop in TRACK Pump
Notes: 17

## Slide 17: Dispense Rate vs. Temperature
Notes: 18

## Slide 18: Temperature Dependence of Resist Viscosity
Notes: 19

## Slide 19: Theory of Spin Coating
Conservation of solvent
Radial momentum/continuity
Can show theoretically that
where
Boundary Conditions
Notes: 20

## Slide 20: Effect of Evaporation on Film Height During Spinning
Notes: 21

## Slide 21: Final Film Thickness: Single Dispense
Notes: 22

## Slide 22: Ultra Casting Predispense Technique
2000
4000
6000
2000
4000
6000
time[sec]
3-5 cc dispense
1cc dispense
time[sec]
EBR
EBR
casting rpm
casting rpm
UCP
conventional dispense
UCP dispense
Note: All dispenses achieve complete coverage of the wafer with coating solution (Resist) ; the process
that forms the final thickness and uniformity is at the same rpm in both cases !
< 1 sec
Notes: 23

## Slide 23: UCP Resist Coating - 2 Layer Model
Layer 1
Layer 2
g
2
wafer
FORCE
g
1
g
2
g
1
<<<
Step 1: (1cc) Overcome surface tension
        Use radial force (ultra casting rpm, 5000-6000 rpm)
        Create interface
Step 2: (1cc) Dispense at or below casting rpm,
        Minimal resist needed because very little resistance
        from surface tension
Solvent Evaporation
Viscous Flow
Notes: 24

## Slide 24: Resist Thickness vs. RPM
560 Resist Thickness vs. RPM
7500
9500
11500
13500
15500
17500
19500
21500
0
500
1000
1500
2000
2500
3000
3500
4000
4500
UCP
5cc
1cc
* Once surface is wetted, only a small additional amount is needed to built thickness.
* Key concept: initial wetting at ultra casting rpm, second dispense at or below casting
rpm
Angstrom
Notes: 25

## Slide 25: Resist Thickness vs. RPM ALL DATA
Notes: 26

## Slide 26: Final Film Thickness: Double Dispense Data
Notes: 27

## Slide 27: Final Height: Single and Double Dispense
Notes: 28

## Slide 28: Conclusions
Resist usage:
  ~5ml for single dispense
  ~2ml for UCP method
Resist thickness and uniformity: identical for both methods
Comparison to theoretical models: identical for both methods; slightly stronger viscosity dependence than predicted theoretically
Resist and solvent usage reduction yields substantial reduction in VOC emissions

## Slide 29: Acknowledgments
Motorola MOS 12
  Tom Roche
  Melissa Masteller
  Frank Fischer
  Michelle Demumbrum
University of Arizona
  Chris Doty
Notes: 39